## Slide 1
Investigation of Stability Trends in Bimetallic CuAg, CuAu, and AgAu Nanoparticles via Bond-Centric Model
Mahmoud Ramadan, James Dean, Jon Estes, Giannis Mpourmpakis (PI)
PFM REU
August 1, 2018
Computer-Aided Nano and Energy Lab (CANELA)
Notes: Instructions for editing school and department titles:
Select from menu: View > Master > Slide Master
Click on each text area you wish to edit. Text will become editable.

## Slide 2: Nanoparticles (NPs)
Nanoparticles: clusters in the nanoscale
High surface to volume ratio
Access to low coordination sites
More control over local chemical environment
Source: Wikimedia Commons
Notes: NP are particles between 1 and 100 nm in size
The human eye can only see up to the micro scale, and can identify strand of hair is about 65 microns or micrometers
Low coordination sites are morereactive than high coordaintion (found in larger metals)

## Slide 3: Applications
  Electronics1
    Integrated circuits and transistors
  Optics1
    Colorings in stained glass
  Catalysis2
    Adsorption
    Activation of molecules
  Medicine3:
    Drug delivery
    Novel drugs
Source: The Scientist. Cover. August 2014.
Source: Wikimedia Commons
Source: Wikimedia Commons
Notes: They have numerous applications in electronics , optics, catalysis , and medicine
Electronics : using silicon-on-oxide
Optics : glass artisans were making stained glass windows from coinage metals

## Slide 4: Cohesive Energy (CE)
Describes bond strength within a NP
Can be used to assess NP stability
Previously-developed Bond-Centric (BC) model1 can cheaply and quickly calculate CE of BNPs
Notes: Cohesive energy is the energy gained or lost by arranging the atoms in a crystalline state, as compared with the gas state
The more negative the cohesive energy, the more stable
Can be used to compare NP of different structures within the same composition
Quantum chemistry methods, such as DFT , are usally used to calculate the energies of NPs, but they are computationally expensive , so instead

## Slide 5: Aims
Investigate composition and morphology of Bimetallic NPs (BNPs)
  Monte Carlo sampling of different NPs
  BC model1 to determine NP stability
Determine preferred chemical ordering in BNP
Overall: Identify most thermodynamically stable BNPs

## Slide 6: Algorithm
Select morphology
Select composition
Calculate CE using BC Model
Assign random chemical ordering

## Slide 7: Methods
Atomic Simulation Environment as implemented in Python to generate BNPs
CE of BNPs was calculated using BC model1
Monte Carlo Sampling
  55- and 147-atom NPs
  Icosahedral and cuboctahedral NPs
  CuAg, CuAu, AgAu
    0-100% dopant, in 5% increments
55-atom BNPs: 350,000 chemical orderings/composition
147-atom BNPs: 1,000 chemical orderings/composition
Notes: ASE Was implemented in python to generate the NP
BC model was used to cheaply and quickly calculate the CE , allowing us to screen 10000s of NPs and determine their

## Slide 8: CE Plot of CuAg
Average CE decreases (more exothermic) as the Cu composition increases in CuAg BNPs
Chart: 147-atom CuAg NP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron | -2.6047 | -2.6189 | -2.634 | -2.6523 | -2.6693 | -2.6867 | -2.7082 | -2.7278 | -2.748 | -2.7723 | -2.7948 | -2.8183 | -2.845 | -2.8699 | -2.8957 | -2.9261 | -2.9535 | -2.9822 | -3.0157 | -3.046 | -3.0815
Cuboctahedron | -2.5272 | -2.541 | -2.5555 | -2.5734 | -2.5894 | -2.607 | -2.6275 | -2.6465 | -2.6662 | -2.69 | -2.7114 | -2.7338 | -2.7604 | -2.7846 | -2.8097 | -2.8389 | -2.866 | -2.8934 | -2.9258 | -2.9553 | -2.9898
Chart: 55-atom CuAg NP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron | -2.4662 | -2.4763 | -2.4924 | -2.5096 | -2.5278 | -2.5406 | -2.5605 | -2.5816 | -2.6037 | -2.6191 | -2.643 | -2.6679 | -2.694 | -2.712 | -2.7398 | -2.7687 | -2.7987 | -2.8193 | -2.851 | -2.8838 | -2.9177
Cuboctahedron | -2.3587 | -2.3684 | -2.3838 | -2.4001 | -2.4176 | -2.4298 | -2.4489 | -2.4691 | -2.4902 | -2.5049 | -2.5278 | -2.5516 | -2.5766 | -2.5938 | -2.6204 | -2.648 | -2.6767 | -2.6963 | -2.7266 | -2.758 | -2.7904

## Slide 9: CE Plot of AgAu
Chart: 55-atom AgAu NP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron | -3.1852 | -3.1662 | -3.1368 | -3.1061 | -3.0742 | -3.0522 | -3.0183 | -2.9832 | -2.9468 | -2.9219 | -2.8835 | -2.8438 | -2.803 | -2.7751 | -2.7322 | -2.6881 | -2.6428 | -2.6119 | -2.5646 | -2.516 | -2.4662
Cuboctahedron | -3.0463 | -3.0282 | -3 | -2.9706 | -2.9401 | -2.9192 | -2.8867 | -2.8531 | -2.8183 | -2.7945 | -2.7577 | -2.7198 | -2.6808 | -2.6541 | -2.6131 | -2.5709 | -2.5276 | -2.498 | -2.4527 | -2.4063 | -2.3587
stdv icosa up | -3.1852 | -3.1654 | -3.1354 | -3.1042 | -3.0719 | -3.0498 | -3.0155 | -2.9801 | -2.9436 | -2.9185 | -2.88 | -2.8404 | -2.7995 | -2.7717 | -2.7289 | -2.685 | -2.64 | -2.6093 | -2.5624 | -2.5144 | -2.4662
Average CE increases (less exothermic) as the Ag composition increases in AgAu BNPs
Chart: 147-atom AgAu NP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron | -3.3641 | -3.3377 | -3.3102 | -3.2777 | -3.2483 | -3.2178 | -3.1817 | -3.1492 | -3.1157 | -3.0759 | -3.0406 | -3.0039 | -2.9611 | -2.9222 | -2.8827 | -2.8364 | -2.7944 | -2.7517 | -2.7018 | -2.6571 | -2.6047
Cuboctahedron | -3.2639 | -3.2383 | -3.2116 | -3.18 | -3.1515 | -3.1218 | -3.087 | -3.0553 | -3.0228 | -2.9844 | -2.9498 | -2.9146 | -2.8726 | -2.8353 | -2.7968 | -2.7517 | -2.7113 | -2.6699 | -2.6213 | -2.578 | -2.5272

## Slide 10: CE Plot of CuAu
Chart: 55-atom CuAu NP
| 100 | 95 | 90 | 85 | 80 | 75 | 70 | 65 | 60 | 55 | 50 | 45 | 40 | 35 | 30 | 25 | 20 | 15 | 10 | 5 | 0
Icosahedron | -2.9177 | -2.9404 | -2.9726 | -3.0026 | -3.0304 | -3.0478 | -3.0719 | -3.0938 | -3.1136 | -3.1256 | -3.1415 | -3.1555 | -3.1671 | -3.1736 | -3.1816 | -3.1874 | -3.191 | -3.1921 | -3.192 | -3.1897 | -3.1852
Cuboctahedron | -2.7904 | -2.8122 | -2.843 | -2.8717 | -2.8984 | -2.9149 | -2.9379 | -2.9589 | -2.9778 | -2.9892 | -3.0046 | -3.0179 | -3.0289 | -3.0352 | -3.0428 | -3.0485 | -3.0519 | -3.053 | -3.0528 | -3.0507 | -3.0463
stedv above icosa | -2.9177 | -2.9325 | -2.9601 | -2.9869 | -3.0122 | -3.0281 | -3.0504 | -3.0708 | -3.0894 | -3.1007 | -3.1161 | -3.1297 | -3.1413 | -3.148 | -3.1566 | -3.1635 | -3.1688 | -3.1714 | -3.1743 | -3.1766 | -3.1852
stedv below icosa | -2.9177 | -2.9482 | -2.985 | -3.0183 | -3.0487 | -3.0675 | -3.0934 | -3.1169 | -3.1378 | -3.1504 | -3.167 | -3.1812 | -3.1929 | -3.1993 | -3.2065 | -3.2113 | -3.2132 | -3.2129 | -3.2098 | -3.2028 | -3.1852
stdev abov cubo | -2.7904 | -2.8014 | -2.8261 | -2.8505 | -2.8738 | -2.8884 | -2.9091 | -2.9281 | -2.9455 | -2.9562 | -2.9707 | -2.9835 | -2.9946 | -3.0012 | -3.0097 | -3.0167 | -3.0223 | -3.0254 | -3.0292 | -3.0333 | -3.0463
stdev below | -2.7904 | -2.8229 | -2.8599 | -2.8929 | -2.923 | -2.9413 | -2.9668 | -2.9897 | -3.0101 | -3.0222 | -3.0385 | -3.0522 | -3.0632 | -3.0692 | -3.076 | -3.0802 | -3.0815 | -3.0806 | -3.0764 | -3.068 | -3.0463
Chart: 147-atom CuAu NP
| 100 | 95 | 90 | 85 | 80 | 75 | 70 | 65 | 60 | 55 | 50 | 45 | 40 | 35 | 30 | 25 | 20 | 15 | 10 | 5 | 0
Icosahedron | -3.0815 | -3.1127 | -3.1421 | -3.1733 | -3.1986 | -3.2224 | -3.2472 | -3.2675 | -3.2861 | -3.304 | -3.3187 | -3.3313 | -3.3434 | -3.3531 | -3.3603 | -3.3657 | -3.369 | -3.3708 | -3.3706 | -3.3689 | -3.3641
Cuboctahedron | -2.9898 | -3.0198 | -3.0484 | -3.0784 | -3.1031 | -3.1256 | -3.151 | -3.1694 | -3.1872 | -3.2061 | -3.2189 | -3.2318 | -3.2442 | -3.2531 | -3.2587 | -3.2664 | -3.2693 | -3.2706 | -3.2699 | -3.2681 | -3.2639
icosa stdev up | -3.0815 | -3.1087 | -3.1367 | -3.1661 | -3.1903 | -3.213 | -3.2374 | -3.2569 | -3.2749 | -3.2925 | -3.3062 | -3.3192 | -3.331 | -3.3413 | -3.3483 | -3.3547 | -3.359 | -3.3617 | -3.3628 | -3.3626 | -3.3641
icosa stdev down | -3.0815 | -3.1167 | -3.1475 | -3.1805 | -3.2068 | -3.2318 | -3.257 | -3.2782 | -3.2973 | -3.3155 | -3.3311 | -3.3433 | -3.3557 | -3.3648 | -3.3723 | -3.3768 | -3.379 | -3.3799 | -3.3785 | -3.3753 | -3.3641
cubocta up | -2.9898 | -3.0136 | -3.0399 | -3.0682 | -3.0914 | -3.112 | -3.1363 | -3.1547 | -3.1716 | -3.1896 | -3.2019 | -3.2147 | -3.2275 | -3.2359 | -3.2433 | -3.2509 | -3.2545 | -3.2578 | -3.2586 | -3.2597 | -3.2639
cubocta down | -2.9898 | -3.0259 | -3.0568 | -3.0886 | -3.1148 | -3.1392 | -3.1657 | -3.1842 | -3.2027 | -3.2225 | -3.2359 | -3.2488 | -3.261 | -3.2703 | -3.2741 | -3.2819 | -3.2842 | -3.2834 | -3.2812 | -3.2765 | -3.2639
Average CE increases (less exothermic) as the Cu composition increases in CuAu BNPs
Notes: There is a minimum , but it doesn’t tell us much on the stability with respect to other compositions so instead

## Slide 11: Excess Energy (EE)
The energy lost or gained when forming nanoalloys
Allows for comparison of NPs of different composition
EE of is

## Slide 12: EE Plot (Metal Mixing)
Chart: 55-atom BNP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron CuAg | 0 | 0.012448 | 0.018921 | 0.024326 | 0.028703 | 0.0385 | 0.041102 | 0.042582 | 0.043077 | 0.050249 | 0.048917 | 0.046557 | 0.043032 | 0.047662 | 0.042427 | 0.036065 | 0.028697 | 0.030665 | 0.02153 | 0.01132 | 0
Icosahedron CuAu | 0 | -0.0093342 | -0.028167 | -0.044813 | -0.05927 | -0.063283 | -0.073979 | -0.082544 | -0.088942 | -0.08752 | -0.090136 | -0.090682 | -0.08892 | -0.082088 | -0.076639 | -0.069124 | -0.05934 | -0.047104 | -0.033613 | -0.017919 | 0
Icosahedron AgAu | 0 | -0.016992 | -0.023484 | -0.028749 | -0.032806 | -0.046813 | -0.048829 | -0.049644 | -0.049211 | -0.06024 | -0.057783 | -0.054103 | -0.049196 | -0.057245 | -0.050326 | -0.042166 | -0.032802 | -0.037872 | -0.026462 | -0.013845 | 0
Cuboctahedron CuAg | 0 | 0.011897 | 0.018094 | 0.023291 | 0.027433 | 0.036832 | 0.039291 | 0.040732 | 0.041138 | 0.048075 | 0.046773 | 0.0445 | 0.041165 | 0.04556 | 0.040531 | 0.03451 | 0.027412 | 0.029373 | 0.020608 | 0.010817 | 0
Cuboctahedron CuAu | 0 | -0.0089358 | -0.026991 | -0.042916 | -0.056797 | -0.06046 | -0.070756 | -0.07895 | -0.08503 | -0.083635 | -0.086262 | -0.08673 | -0.084994 | -0.078457 | -0.07329 | -0.06614 | -0.056798 | -0.045103 | -0.03209 | -0.017168 | 0
Cuboctahedron AgAu | 0 | -0.016992 | -0.023484 | -0.028749 | -0.032806 | -0.046813 | -0.048829 | -0.049644 | -0.049211 | -0.06024 | -0.057783 | -0.054103 | -0.049196 | -0.057245 | -0.050326 | -0.042166 | -0.032802 | -0.037872 | -0.026462 | -0.013845 | 0
Chart: 147-atom BNP
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
Icosahedron CuAg | 0 | 0.0096767 | 0.018377 | 0.023998 | 0.030849 | 0.037286 | 0.039576 | 0.043836 | 0.047432 | 0.04696 | 0.048309 | 0.048677 | 0.045807 | 0.044719 | 0.042821 | 0.036256 | 0.032666 | 0.027778 | 0.018197 | 0.011681 | 0
Icosahedron CuAu | 0 | -0.017019 | -0.032284 | -0.049386 | -0.06052 | -0.070223 | -0.08092 | -0.087106 | -0.091544 | -0.09533 | -0.095836 | -0.094323 | -0.092282 | -0.087876 | -0.080948 | -0.072262 | -0.061437 | -0.049065 | -0.03481 | -0.018979 | 0
Icosahedron AgAu | 0 | -0.011541 | -0.022025 | -0.027543 | -0.036053 | -0.043555 | -0.045451 | -0.050908 | -0.055314 | -0.053554 | -0.056161 | -0.057467 | -0.05262 | -0.051645 | -0.050171 | -0.041801 | -0.037806 | -0.033103 | -0.02116 | -0.014406 | 0
Cuboctahedron CuAg | 0 | 0.0093051 | 0.017934 | 0.023132 | 0.030279 | 0.035861 | 0.038433 | 0.042566 | 0.046006 | 0.045326 | 0.047107 | 0.047853 | 0.044328 | 0.043255 | 0.041286 | 0.035199 | 0.031225 | 0.026998 | 0.017771 | 0.01135 | 0
Cuboctahedron CuAu | 0 | -0.016272 | -0.031154 | -0.047519 | -0.058477 | -0.067275 | -0.079001 | -0.083715 | -0.087749 | -0.092933 | -0.092056 | -0.09121 | -0.089965 | -0.08514 | -0.076997 | -0.07101 | -0.060227 | -0.047769 | -0.033398 | -0.017915 | 0
Cuboctahedron AgAu | 0 | -0.011172 | -0.021343 | -0.026619 | -0.034888 | -0.042095 | -0.044111 | -0.049194 | -0.053574 | -0.052055 | -0.054289 | -0.055843 | -0.050747 | -0.050265 | -0.048556 | -0.040372 | -0.036774 | -0.032171 | -0.020443 | -0.013983 | 0
Thermodynamically disfavorable formation of CuAg 55- or 147-atom icosahedral and cuboctahedral BNPs
Favorable formation of 55- and 147-atom CuAu and AgAu icosahedral/cuboctahedral BNPs

## Slide 13: Predicted Structures
Minimum-energy structures of the 55- and 147-atom cuboctahedral and icosahedral 50/50 CuAu and 50/50 AgAu BNPs
Cu
Ag
Au

## Slide 14: Summary
Investigated BNP stability using BC model1
Compared different chemical orderings within the same composition
Identified the favorable formation of 55- and 147-atom icosahedral/cuboctahedral CuAu and AgAu BNPs
Future Work: Incorporate symmetry operations to simulate BNPs of larger size and to decrease the search space

## Slide 15: Acknowledgement
Everyone at CANELA
Dr. Michail Stamatakis (University College London)
Dr. Tayrn Bayles and Dr. Joe McCarthy
Grant Number CMMI-1634880
Grant Number ECC-1659324

## Slide 16
Questions ?